item: 	_______________	material:	_______________________

curve:	_______________	required MDMT:	_______________________

governing thickness as defined in UCS-66(a):	_______________________

| UG-20 (f) | No | Yes | exempted from Impact Testing |
| --- | --- | --- | --- |
| 1 | P-No. 1 Material Gr. No. 1 or 2 | ( | ( |  |
| 2 | governing not exceeding: Curve A material: ½ in (12,7mm) Curve B, C, D material: 1 in. (25,4mm) | ( | ( |  |
| 3 | complete vessel hydrostatically tested | ( | ( |  |
| 4 | design temperature not warmer than 650 °F (343°C) | ( | ( |  |
| 5 | MDMT not colder than –20°F (-29°C) | ( | ( |  |
| 6 | thermal or mechanical shock loadings or cyclical loading are not controlling design requirements | ( | ( |  |
|  | all requirements (1-6)are met: | ( | ( |  |
|  |  | ( | ( |  |
| UCS-66 (a) | No | Yes |  |
| minimum design metal temperature (MDMT) and thickness combination is on or above the curve in Fig. UCS-66 (or equal or above the values given in Table UCS-66) | ( | ( |  |
|  | ( | ( |  |
| UCS-66 (b) Ratio: tr · E / (tn – c) = ________________________ = __________ tr : required thickness (corroded) for all applicable laodings E : joint efficiency [ref. general note (3), but not less than 0.8] tn : nominal thickness (not corroded) c : corrosion allowance As an alternative, the ratio of MAWP and max. allowable pressure may be used. Ref. UCS-66(i) reduction of MDMT: _______________ MDMT from Fig. UCS-66: _______________ reduced MDMT: _______________ May not be colder than –55°F (-48°C), except as per UCS-66(b)(3) | No | Yes |  |
| MDMT from Fig. UCS-66 for the specified nominal thickness minus reduction from UCS-66 (b) colder than required MDMT | ( | ( |  |
|  | ( | ( |  |
| Exempted due to: | No | Yes |  |
| UCS-66(c), (d), (g), (h) or reduction of MDMT by UCS-66(i) | ( | ( |  |
|  | ( | ( |  |
| Impact Testing required in accordance with UG-84 |